## Slide 1: Negative muons for Heritage Science: background and applications
Matteo Cataldo, Phd
MELODY, CSNS
11/01/2024

## Slide 2
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Agenda
Introduction: scientific background
Research with negative muons: activities @ Milano Bicocca
Conclusions
2

## Slide 3
About me: research fellow @ Milano Bicocca
University of Milano Bicocca
ISIS Neutron and Muon Source
Max
Aidy
Me!
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
3
Notes: I’m a former facility development phd student at the ISIS Neutron and muon source, with a cofunded phd project with the university of milano bicocca

## Slide 4: Introduction: negative muon interaction with matter
Capture generally occurs at n ≈ 14;
First part of the cascade: Auger emission;
From n ≈ 6, characteristic radiative X-ray emission becomes dominant (elemental analysis);
The muon reaches the 1s state: decay or capture by the nucleus;
When a µ- interacts with matter, a “Muonic atom” is formed1
Muonic atom X-ray Emission spectroscopy (µ-XES)
is the technique based on the detection of these high energy radiation
1 Hillier, A.D., Blundell, S.J. et al. Nat Rev Methods Primers 2, 4 (2022). https://doi.org/10.1038/s43586-021-00089-0
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
4
Notes: Muon is slowed down and captured by the coulomb field of the nucleus
outer atomic electrons of the atom until it is captured by the Coulomb field of the nucleus.
Due to the mass of the muon, it will orbit 207 times closer to the nucleus, thus experiencing
207 times higher binding energies.

## Slide 5: Introduction: negative muon interaction with matter
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
5

## Slide 6: Introduction: negative muon interaction with matter
When a µ- interacts with matter, a “Muonic atom” is formed1
If captured:
The daughter will be an exited Z-1 nuclei;
De-excitation via the emission of neutrons and gamma rays.
In addition, during the cascade:
6. Due to the rearrangement of the structure, electronic X-ray close to the Z-1 species can be observed
7. After capture, delayed electronic X-ray of the Z-1 species
Used to understand the cascade process dynamics.
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
6
1 Hillier, A.D., Blundell, S.J. et al. Nat Rev Methods Primers 2, 4 (2022). https://doi.org/10.1038/s43586-021-00089-0
Notes: Hence, the reaction produces an exited Z-1 nuclei that will deexcite via the emission of neutrons and gamma rays. These gamma rays can be used for isotope identification since they are characteristic of the emitting species

## Slide 7: Introduction: µ-XES – Why?
m = 105.7 MeV/c2
Multi-elemental
Remarkable penetration depth Momentum & Density dependent
Non-invasive probe
No activation of samples
Negligible self-absorption effect
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
7
Notes: 1 cm in copper and silverWhy muon have remarkable penetration depth (if compared to electron)
Different interaction, energy is lost by ionization and radiation instead of brehmstralung
Thanks to the mass, they are less effected by electromagnetic forces
Smaller cross section than electrom, less likely to interact
. Being able to probe non-destructively a lithium battery, will enable a better understanding of the mechanism and limiting factors for battery dis(re) charge.

## Slide 8
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Introduction: µ-XES – Literature (for Heritage Science)
8

## Slide 9: Introduction: µ-XES at ISIS
MuX Port4 Setup @ RIKEN RAL
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
9
Notes: Where it is performed

## Slide 10
M. Cataldo, NMUSM Meeting, Warwick, 19th April 2023
Gildings
Bronze artefacts
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Research activities at Milano Bicocca: Archaeometry
Enamels
10

## Slide 11
Characterization of thin layers with negative muons
Develop a protocol for an improved interpretation of negative muon data, especially for multi-layerd artefacs
By using simulation software that can be used to replicate an experiment
Software: SRIM-TRIM & GEANT4/ARBY
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
How?
By comparing the result of measurement and simulation, the size of a given layer is addressed
11
Notes: Main focus, started with gold now with enamels
Over the years, experiments were performed without a clear idea from users on how to use the collected data (and a PhD student that worked on the anlaysis )

## Slide 12
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Characterization of thin layers with negative muons
12

## Slide 13
To finally give a
depth profile
The intensity of the X-rays varies as the muon beam momentum changes
From that, the variation of the composition of the layer is reconstructed
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Characterization of thin layers with negative muons
13

## Slide 14
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Characterization of thin layers: gildings
14

## Slide 15
«Annunciation to Zachary» Andrea Pisano, Leonardo D'Avanzo e bottega (1329 -1336)
(Courtesy of F. Cantini – CNR-IFAC)
Validation process: from mockup samples to a real bronze sample
Mockup sample
Top: SM3, Bottom: EM2
(dimensions:.5cmx2.5cmx0.5cm)
Mockup sample
(dimensions:5cmx5cmx0.0005cm)
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Characterization of thin layers: gildings
15

## Slide 16
10.4 µm
3.7 µm
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Characterization of thin layers: gildings
16
Validation process: from mockup samples to a real bronze sample

## Slide 17
Sample A
Average gold thickness form SEM: 3.3 ± 0.2 μm
Measured gold thickness: 3.5 ± 0.5 μm
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Characterization of thin layers: gildings
17

## Slide 18
Sample C
Average gold thickness form SEM: 7.3 ± 0.8 μm
Measured gold thickness: 7.5 ± 0.5 μm
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Characterization of thin layers: gildings
18

## Slide 19
Angel body: gold thickness of 16 ± 0.5 μm
Zachary body: gold thickness of 15 ± 0.5 µm
Lion: gold thickness of 15 ± 0.5 µm
Good control of the process gilding process
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Characterization of thin layers: gildings
19

## Slide 20
Painted enamels: preliminary study on mockup samples
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Characterization of thin layers: Enamels
20
Notes: APPLY SAME APPROACH TO OTHER MATERIALSThe city of Limoges, in the south-west of France, has been the centre of production of enamels since the Middle Ages. Enamels consist of thin layers of glass, coloured by a metallic compound fused on a metal surface. Their quality was so fine that they were compared to paintings: a copper layer as a canvas and the glass as the paint, representing mostly mythology and religion scenes (Figure 1). The production covered three centuries, from XV to XVII, with a renewed interest in the XIX century. Enamels can be manufactured using different techniques (champlevé or cloisonné for example) but what is peculiar of the Limoges painted enamels, is that they are characterized by a multi-layered structure, done by consecutive firing steps. The colour was guaranteed by the presence of different chromophores, apart from the “en grisaille” technique, were only black and white was used.

## Slide 21
µXES could be one of the only techniques that can probe beneath the surface and perform a non-destructive quantitative analysis of painted glasses.
Enamels represent a challenge for conservation scientists:
Very fragile artefacts: sampling could cause damage and should be avoided
Layers can be in the order of the hundreds of microns
The glass can be altered on the surface: muons could provide quantitative information from the bulk of the material
Alteration
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Characterization of thin layers: Enamels
21

## Slide 22
Preliminary results (beamtime @ISIS in October 2024)
PRELIMINARY
PRELIMINARY
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Characterization of thin layers: Enamels
22

## Slide 23
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
CHNet-MAXI (Muonic Atom X-ray spectroscopy for Isotopic analysis) project: aims at developing a reliable system for isotopic analysis with µ-XES for cultural heritage (2023-2025 purposes.
Research activities at Milano: facility development
A muon beam hodoscope to be used as a beam x/y profiler and a beam intensity monitor
A set of scintillating detectors read by SiPM for a compact detection system (GAGG and CLLB)
Array of 9 Hpge and customized acquisition system based on CAEN Digitizers
Main features:
23

## Slide 24
Conclusions & future work
谢谢各位的聆听!
µ-XES has unique characteristics among the many other elemental technique in the field of cultural heritage:
    Sensitive to (almost) all elements
    Depth selective
    Non-destructive
Combined with Monte Carlo simulations, Muonic X-ray spectroscopy can be used to address the size of thin layers in materials.
This approach is still a work in progress, but results are promising. In the future I will continue the work with enamels and to improve the capabilities of thesimulation software .
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025

## Slide 25
For the SM3 sample, the results are in agreement with the measurements but also with the SEM results (11 ± 0.5 μm). While for the EM2 sample, a different thickness has been evaluated (5 ± 0.5 μm).
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Characterization of thin layers: gildings

## Slide 26
M. Cataldo – Negative muons for Heritage Science: background and applications, MELODY, CSNS 11/01/2025
Research activities at Milano: facility development